Table 1 Nominal and actual phen contents, structural parameters, specific surface areas, and optical band gap values of the organoceria nanostructured hybrid materials and the phen-free CeO2 NCs control sample.

| Sample | Nominal phen content / wt.% | phena / wt.% | Db / nm | Dc / nm | d(111)d / nm | SBETe /m2·g-1 | Egf / eV |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CeO2 NCs | - | - | 46.5 | 47.0 | 0.31 | 20.5 | 3.23 |
| CeO2 NCs_ Phen-0.04 | 4.2 | 0.9 | 38.7 | 40.3 | 0.31 | 27.8 | 3.17 |
| CeO2 NCs_ Phen-0.08 | 8.0 | 1.8 | 25.5 | 27.3 | 0.31 | 29.5 | 3.11 |

a Actual phen content from TG analyses.

b Average crystalline domain size as estimated from PXRD.

c Mean particle size as determined from STEM.

d Ceria lattice spacing from PXRD.

e Specific surface area from N2 adsorption/desorption isotherms.

f Band gap energy as calculated from Tauc plot.

Table 2 Comparison of the photocatalytic hydrogen production performance of representative ceria-based materials with and without co-catalysts.

| Sample mass / mg | Co-catalyst | Reducing agent | Power of light source / W | λ / nm | H2 yield / μmol·(g·h)-1 | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| 10 | Pt | Ethanol | 450 | > 200 | 153.0 | This work |
| 30 | - | Methanol | - | > 400 | 68 | 1 |
| 50 | - | - | 400 | > 200 | 12.5 | 2 |
| 1000 | - | - | 450 | > 200 | 7.1 | 3 |
| 1000 | Pt | - | 450 | > 200 | 7.7 | 3 |
| 1000 | Li | - | 450 | > 200 | 8.4 | 3 |
| 1000 | Cs | - | 450 | > 200 | 81.6 | 3 |
| 100 | - | Na2S + Na2SO3 | 300 | > 200 | 5.0 | 4 |
| 10 | - | Ethanol | 225 | > 200 | 112 | 5 |

References

1	Y. Huang, C.-F. Yan, C.-Q. Guo and Y. Shi, Int. J. Hydrogen Energy, 2016, 41, 7919–7926.

2	J. Krishna Reddy, G. Suresh, C. H. Hymavathi, V. Durga Kumari and M. Subrahmanyam, Catal. Today, 2009, 141, 89–93.

3	K.-H. Chug and D.-C. Park, Catal. Today, 1996, 30, 157–162.

4	B. Dong, L. Li, Z. Dong, R. Xu and Y. Wu, Int. J. Hydrogen Energy, 2018, 43, 5275–5282.

5	A. S. Thill, F. O. Lobato, M. O. Vaz, W. P. Fernandes, V. E. Carvalho, E. A. Soares, F. Poletto, S. R. Teixeira and F. Bernardi, Appl. Surf. Sci., 2020, 528, 146860.